Technical Specification

All work shall be carried out in accordance with the Specification of Building and Road Works – 2025 and the specifications mentioned herein;

- Providing and laying PVC pipes and fittings

The work shall include supplying, laying, jointing, testing and commissioning of PVC piping system complete with fittings, supports, clamps and all accessories for soil, waste, and vent lines as per drawings and specifications.

- Materials

PVC SWR pipes shall be Type B (heavy duty) confirming with IS 13592. The recommended brands are Astral, Supreme, or any equivalent brand.

- Jointing Procedure

Rigid PVC joint shall be carried out using the manufacturer-recommended solvent cement. Clean pipe and fittings with a dry cloth and apply approved PVC solvent cement evenly on both surfaces. Insert pipe fully into socket and hold for 30 seconds, then wipe excess cement. Allow a curing time of a minimum of 24 hours before handling rough.

Rubber ring/ push fit joint shall be carried out using manufacturer recommended lubricant. Clean socket and spigot and apply approved pipe lubricant on rubber ring and pipe end. Insert pipe fully up to marked depth ensuring current alignment.

- Laying & Alignment

Pipes shall be laid true to line and level with a minimum slope of 1 in 60, ensuring self cleansing velocity to avoid choking.

- Testing & Inspection

Check alignment and slope before joining. Conduct a water test by filling the pipe and check for leakage.

- Installation of floor & wall tiles.

This specification covers the supply, handling, and installation of vitrified tiles for floor and wall surfaces, including all related adhesives, grouts, leveling, joint finishing, and protection during construction.

- Materials

The vitrified tiles (glazed/full-body polished/double-charged, depending on the design) shall be used. The 450x450mm tiles with a minimum thickness of 10mm and anti-skid tiles shall be used for the floor, and the 600x600mm tiles with a minimum thickness of 8mm shall be used for the wall. The color/ finish of the tiles shall be approved by the supervising engineer.

- Installation

To maintain the uniform joint width and to avoid lippage, appropriate spacers shall be used. The joint width shall be 2 mm, and it shall be sealed with manufacturer-recommended epoxy-based sealant. The minimum slope of 1 in 100 towards the drain shall be maintained.

Installation of sanitaryware.

All sanitaryware shall conform to the specification tabulated below. The installation shall be carried out as per the manufacturer's instructions.

| Brand: Hindware |  |  |
| --- | --- | --- |
| SN | Name | Code |
| 1 | Elna under-counter basin | S48IE1S0N |
| 2 | Prima WD One Piece Toilet - S 220 | 92665 |
| 3 | Starc Health Faucet | F160194CP |
| 4 | Edge pillar cock | F410001 |
| 5 | Bottle trap 32mm with 125mm & 175mm lengths | F850015 |
| 6 | Smart with SP | 60011 |
| 7 | Wall Hung Urinal Division | SU81OSC-C-STD-CR |
| 8 | Exposed part kit concealed stop cock 20mm | F400027 |

- Application of Dr. Fixit Bathseal Select

- Prepare the substrate by thoroughly cleaning the surface and repairing all cracks, honeycombs, and other defects. Apply Dr. Fixit Bathseal in two coats (in a perpendicular direction to the previous coat), or as recommended by the manufacturer, over the entire toilet floor and extend the waterproofing at least 300 mm up the walls. After the waterproofing has cured, conduct a 24–48-hour ponding test to verify that the treated area is completely watertight. Upon successful completion of the ponding test, proceed with laying the floor and wall tiles using a suitable tile adhesive or cement-sand mortar, ensuring that the waterproofing membrane is not damaged during subsequent finishing works.

- Providing and fixing Greenlam Sturdo Essentia Collection – Serene Restroom Cubicle of standard dimensions, fabricated from 12 mm thick compact high-pressure laminate (HPL) panels conforming to IS 2046, EN 438, and NEMA LD3 standards, with antibacterial, antiviral, antifungal, and Greenguard Gold certified properties. The work shall include supply and installation of all necessary nylon polyamide and powder-coated aluminium hardware, including self-closing hinges, thumb-turn lock, coat hook, adjustable legs, U/F profiles, top rail, rubber buffers, SS 316 screws, wall plugs, and all accessories complete. Cubicles shall be installed with 150 mm floor clearance, complete in all respects as per the manufacturer's specifications, approved drawings, and the Engineer's instructions.